# Text boxes

Name of the module: Physical properties of nanomaterials for energy applications

Number of module: 365 - 2 - 9609

BGU Credits: 3

ECTS credits: 6

Academic year: 2012- 2013

Semester: Spring

Hours of instruction: 3 lecture hours per week

Location of instruction: will be defined.

Language of instruction: Hebrew

Cycle: First cycle

Position: an advanced course for graduate students of Materials Engineering Department

Field of Education: Materials Engineering

Responsible department: Materials Engineering

General prerequisites: Nonew

Grading scale: the grading scale would be determined on a scale of 0 – 100 (0 would indicate failure and 100 complete success 0 to 100), passing grade is 75.

Lecturer: Dr. Shmuel Hayun

Contact details: room 019, building 63

Office phone: 08- 6428742

Email: hayuns@exchange.bgu.ac.il

Office hours: Monday, from 8 to 11 AM.

Module evaluation: at the end of the semester the students will evaluate the module, in order to draw conclusions, and for the university's internal needs.

Course Description:

Aims of the module: Students will expand their knowledge on the physical properties of nanomaterials, characterization methods, and measurement techniques and errors treatment.

Objectives of the module: To familiarize students with modern techniques and to expand their understanding of principles and theory of these methods.

Learning outcomes of the module: On successful completion of the course, the students should be able to:

  - Described and define the unique properties of nanomaterials? (size effects on physical and chemical properties)

  - How to characterize nanometer materials? (X-ray diffraction, small angle X-ray diffraction (SAXS), electron microscopy (TEM, SEM, AFM), spectroscopy RAMAN, IR and NIR).

  - How the size affect the physical properties in nanomaterial’s? (Heat capacity, melting temperature, lattice constants, electrical properties and mass transfer, surface and interfacial energies, adsorption energies).

  - Understanding the experimental methods capabilities and limitations for physical properties determinations. (calorimetry, LFA, adsorption isotherms )

  - How to asses experimental errors? (statistical methods)

Confirmation: the syllabus was confirmed by the faculty academic advisory committee to be valid on 2012-2013.

Last update: 26 January 2014

Attendance regulation: attendance and participation in class is mandatory (at least 80%).

Teaching arrangement and method of instruction: The module consists of lectures.

Assessment:

- Exercises 50%

- Work & Presentation 50%

Work and assignments: will be defined during the class

Exam: at the end of semester, open and closed questions.

Time required for individual work: in addition to attendance in class, the students are expected to do their assignment and individual work: at least three hours per week.

Module Content\ schedule and outlines:

| Week | Subject | Time |
| --- | --- | --- |
| 1 | Introduction to nanomaterial | 3h |
| 2 | Physical chemistry of solid surfaces | 3h |
| 3 | Nanoparticles synthesis | 3h |
| 4-5 | Characterization methods | 6h |
| 6 | Students presentations | 3h |
| 7-8 | Physical properties determination | 6h |
| 10 | Experimental work in the lab | 3h |
| 11 | Experimental methods capabilities | 3h |
| 11 | Students presentations | 3h |
| 12 | Experimental error treatment | 3h |
| 13 | Summary and integration of all methods to gain a complete picture | 3h |

Exercises:

Required reading:

  - Guo-Zhong Cao, Ying Wang, Nanostructures and Nanomaterials: Synthesis, Properties, and Applications (2Nd Edition) World Scientific, 2011 - 581 pages

  - Yury Gogotsi, Nanomaterials Handbook, CRC Press 2006 -800 Pages

  - Taylor, John Robert, An Introduction to error analysis: the study of uncertainties in physical measurements. Oxford :University Science Books, 1982.

Additional literature: